September 23, 2008

Testing was performed in accordance with:

ASCE 19-96, 3.2.2., which requires fittings to develop an ultimate strength of at least 110% of the specified nominal cable strength.

| Work Order No.: | 235706-016 | Lot No.: | 235706-016 | Date: | 10/3/06 |
| --- | --- | --- | --- | --- | --- |
| BRACE-GRIP® DE CAT NO. | STRAND SIZE (in.) | STRAND MBS (lbs.) | MAXIMUM LOAD (lbs.) | % MBS | FAILURE MODE AT MAX. LOAD |
| BRG-2587 | 5/8" EHS G.S. | 42,400 | 46,799 | 110.4 | Sample failed midspan at max. load. |
|  |  |  | 46,200 | 109.0 | Big Grip DE faiiled at ram end, Brace-Grip DE did not fail. |
|  |  |  | 47,100 | 111.1 | Strand failed midspan at max. load. |
|  |  |  | 47,300 | 111.6 | Big Grip DE failed in loop at max. load. |
| AVERAGE |  |  | 46,849.75 | 110.7 |  |

Regards,

Scott L. Sanderson

Corporate Quality Assurance Engineer

ma

cc:  File 94

J. Reilly